SEISMIC PERFORMANCE OF SHEAR DEFICIENT EXTERIOR RC BEAM-COLUMN JOINTS REPAIRED USING CFRP COMPOSITES

Y. A. Al-Salloum, S. H. Alsayed, T. H. Almusallam and N. A. Siddiqui

Department of Civil Engineering, KSU, P.O. Box 800, Riyadh, Saudi Arabia

ABSTRACT

In this paper, efficiency and effectiveness of using Carbon Fiber Reinforced Polymers (CFRP) sheets in repairing and upgrading the shear strength and ductility of seismically deficient exterior beam-column joint has been studied. For this purpose, a reinforced concrete exterior beam-column sub-assemblage was constructed with non-optimal design parameters (inadequate joint shear strength with no transverse reinforcement) representing pre-seismic code design construction practice of joints and encompassing the vast majority of existing beam-column connections. The specimen was subjected to cyclic lateral load histories so as to provide the equivalent of severe earthquake damage. The damaged specimen was repaired using CFRP sheets and then subjected to the similar cyclic lateral load history and its response history was obtained.  Response histories of the specimen before and after repair were then compared.  The results were compared through hysteretic loops, load-displacement envelops, ductility and stiffness degradation. The comparison shows that CFRP sheets improve shear resistance and ductility of the joint substantially.

KEYWORDS

Beam-column joints, exterior joint, CFRP, seismic, retrofitting, repair, cyclic loads.

INTRODUCTION

Majority of the pre-1970 constructed reinforced concrete (RC) frame buildings existing across the world and within the Kingdom of Saudi Arabia are shear deficient as they were constructed before the introduction of Seismic Code for construction. Recent earthquakes have illustrated that inadequate shear reinforcement in the existing beam-column joints, especially exterior ones (Figs.1a and 1b), is the prime cause of failure/collapse of moment resisting RC frame buildings.  Hence, effective and economical rehabilitation techniques to upgrade joint shear-resistance in existing structures are needed. In the past, variety of techniques have been employed to upgrade shear capacity and ductility of RC joints, with the most common being construction of RC or steel jackets. Plain or corrugated steel plates have also been tried. These techniques cause various difficulties in practical implementation at the joint, namely intensive labor, artful detailing, increased dimensions, corrosion protection and special attachments. To overcome the difficulties  associated with these techniques, recent research efforts have focused on the use of epoxy-bonded FRP sheets or strips with fibers oriented properly so as to carry  tension forces due to shear.

Figure1a. RC building frame showing an exterior joint.

Figure 1b. A failed exterior joint (Turkey Earthquake, August 1999).

In the last four decades several research papers have been published on the effect of seismic loads on poorly detailed reinforced concrete beam-column joints, typical of pre-seismic code designed moment resisting frames. Pantazopoulou and Bonacci [1], Cheung et al. [2], Pantazopoulou and Bonacci [3], Hakuto et al. [4], Hwang and Lee [5], Baglin and Scott [6] are some of the important contributions.  The research papers, however, on FRP repaired/upgraded beam-column joints are limited.  Antonopoulous and Triantafillou [7] conducted a comprehensive experimental program through 2/3-scale testing of 18 exterior joints.  Their study demonstrated the role of various parameters, e.g. area fraction of FRP, distribution of FRP etc, on shear strength of exterior joints. They also highlighted the importance of mechanical anchorages in limiting premature debonding. Ghobarah and Said [8], El-Amoury and Ghobarah [9] developed an effective selective rehabilitation scheme for RC beam-column joints using advanced composite materials. Mukherjee and Joshi [10] studied experimentally the effect of FRP in improving shear strength and ductility of RC beam-column joints under simulated seismic forces. Ghobarah and El-Amoury [11] developed effective rehabilitation systems to upgrade the resistance to bond-slip of the bottom steel bars anchored in the joint zone and to upgrade the shear resistance of beam-column joints.

A detailed review of literature shows that systematic studies to determine the behavior of the FRP repaired/upgraded members under cyclic loading are still limited. Moreover, the behavior of seismically excited FRP repaired beam-column joints is not well established at various stages of response e.g. before and after yielding of reinforcements, crushing of concrete, fiber fracture or debonding. The present paper is also an effort in the same direction. In this paper, efficiency and effectiveness of Carbon fiber reinforced polymers (CFRP) in repairing and upgrading the shear strength and ductility of seismically deficient exterior beam-column joint has been studied. For this purpose, a reinforced concrete exterior beam-column sub-assemblage was constructed with non-optimal design parameters (inadequate joint shear strength with no transverse reinforcement) representing pre-seismic code design construction practice of joints and encompassing the vast majority of existing beam-column connections. The specimen was subjected to cyclic lateral load histories so as to provide the equivalent of severe earthquake damage. The damaged specimen was then repaired using CFRP sheets. This repaired specimen was subjected to the similar cyclic lateral load history and its response history was obtained.  Response histories of the specimen before and after repair were then compared.  The results were compared through hysteretic loops, load-displacement envelops, ductility and stiffness degradation.

EXPERIMENTAL PROGRAM

Test Specimens

In finding out the size of exterior joint specimen, first a prototype member size was chosen and then a crude analysis was carried out to come up with the most reasonable scale for the test specimen that comply with the available testing facility and equipment.  Half-scale beam-column joint was found to be the most convenient.  The dimensions and details of the half-scale test specimen are shown in Fig. 2a. The specimen was constructed with no transverse reinforcement (Fig. 2b), representing pre-seismic code design construction practice of joints and encompassing the vast majority of existing beam-column connections.

Having decided the size of the test specimen, a reinforced concrete joint specimen was cast. The specimen was then subjected to cyclic lateral load histories so as to provide the equivalent of severe earthquake damage. The damaged specimen was then repaired through injecting epoxy into the cracks and externally bonding the specimens with CFRP sheets, as shown in Figs. 3a and 3b.

Figure 2a. Schematic diagram of exterior joint specimen.

Figure 2b. Reinforcement details of the specimen.

Test Setup

The specimens were tested using the testing apparatus designed and installed in the Structural Test Hall, Department of Civil Engineering, King Saud University, Saudi Arabia.  To apply the simulated seismic type cyclic load on the specimen, a 500-kN servo-controlled hydraulic actuator was connected to a reaction steel frame as shown in Fig. 4. The bottom of the column surface was attached to a base pivot using 4 high strength threaded rods.  The base pivot, in turn, was fastened to a strong steel I-beam.  The latter was post-tensioned to the lab floor using high strength post-tensioning rods.  The rigid end of the concrete beam was tied to rigid link through steel pivots.

(1) Layer of CFRP Sheet all around the Column Section

(Length = 105 cm & Width = 30 cm)

(1) Layer of CFRP Sheet all around the Column Section

(Length =105cm & Width =30 cm)

R/C Column

R/C Slab

R/C Beam

30 cm

30 cm

Rigid Beam End

Top Box

Figure 3a. Schematic representation of FRP repaired specimen.

Figure 3b. Picture showing FRP repaired specimen.

Testing Procedure

To test the specimens horizontal-loading regime was used. The said loading was based on the conventional guidelines of quasi-static type testing as followed by most researchers in simulating seismic forces to test reinforced concrete structures.  The loading cycles were controlled by the peak displacement until failure.  For each displacement level, three fully reversed cycles were completed.  It is important to note that the frequency of applied load (or induced displacement) was maintained constant throughout the test program; it was picked up to be around one cycle per minute, which corresponds to a frequency of 0.0167 hertz.  All cycles were started with the pull direction first then went into the push direction.

Figure 4. Schematic diagram showing the test set up for exterior connection specimens.

DISCUSSION OF TEST RESULTS

In the present section, through various experimental results, the effectiveness of CFRP in improving the as-built joint shear strength and ductility has been studied. The results are presented and discussed under the head of general behavior, hysteretic loops, load-displacement envelopes and stiffness degradation.

General Behavior

Figure 5 shows the general response of joint specimen under lateral cyclic loading. This figures shows that during the displacement controlled loading stages; significant X-shear cracks appeared in the specimen almost symmetrically on both faces of the joint. The shear cracks initiated in diagonal directions and propagated towards the ends of joint. This may be attributed to diagonal tension caused due to excessive shear stresses in the joint.

Having completed the tests on above specimen, the damaged specimen was repaired through injecting epoxy into the cracks and externally bonding the specimens with   CFRP sheets (Fig. 3). Externally bonded CFRP sheets were expected to provide shear resistance to the joint which in turn may add strength and ductility to the joint. It was observed that use of CFRP sheets delayed shear failure of the joint significantly and failure was primarily due to debonding and tearing of CFRP sheets in the beam region (Fig. 6). This is due to the fact that at higher stages of loading, there was significant yielding in beam reinforcing steel bars that allowed cracks to widen in the beam region which in turn ultimately tore the CFRP sheets.

Figures 5. Development of cracks in the exterior RC beam-column joint specimen.

Tearing and de-bonding

Figure 6. Failed FRP repaired exterior beam-column joint specimen.

Hysteretic Behavior

The hysteretic behavior of exterior joints was examined in terms of shear strength (measured in terms of ultimate load) and deformation capacity. The load-displacement relationships for specimens before and after the repair are shown as hysteretic curves in Figs. 7 and 8. Fig. 8 shows that the ultimate load for repaired specimen is substantially higher than its corresponding original (before repair) specimen (Figs. 7 and 8). This is primarily due to the increased confinement of joint resulting from externally bonded CFRP sheets. A further comparison of deformation capacity of repaired specimens with the original (i.e. before repair) specimen illustrates that the use of CFRP increases the deformation capacity of repaired specimens considerably.

Figure 7. Load-displacement hysteretic plot for original (before repair) specimen.

Figure 8. Load-displacement hysteretic plot for repaired specimen.

Load-Displacement Envelopes

In order to study load carrying capacity and ductility of original (before repair) and repaired exterior joint specimens, envelopes of load-displacement hysteretic curves for these two specimens are plotted and shown in Figure 9. Using these envelopes the peak load, ultimate displacements, and ductility for the specimens are obtained and listed in Table 1.  The second column of Table 1 shows the average peak load (i.e. average of peak push and pull values) and third column shows the displacement corresponding to first yield of steel bars. This displacement is required to calculate ductility of the specimens. The estimated ductility, an important parameter for earthquake resistant construction, is shown in the last column of Table 1. The ductility is computed as the ratio of ultimate displacement to the displacement at first yield of internal steel. For computation, the ultimate displacement was set at a displacement corresponding to 20% drops of peak load. The values of ductility clearly show that the application of CFRP sheets has improved the ductility of repaired specimen significantly. This increase in the ductility is up to 39% with respect to the before repaired specimen.

Table 1: Peak test load and maximum ductility

| Specimen | Peak load (Average) kN | Disp. at first yield of steel, Δy(mm) | Disp. at 20% drop of peak load, Δ20 (mm) | Ductility Factor Δ20Δy |
| --- | --- | --- | --- | --- |
| Before repair | 47.08 | 18.67 | 30.0 | 1.61 |
| After repair | 81.79 | 18.67* | 40.7 | 2.24 |

*Taken same as respective “before repair” values.

Table 1 illustrates that the increase in average peak load for repaired specimen is substantially higher than the original (before repair) as-built specimen by 74%. This is highly encouraging trend and may be attributed to excellent performance of CFRP sheets attached to the damaged specimen.

Figure 9. Envelope of hysteretic loops.

The ductility, an important parameter for earthquake resistant construction, is shown in the last column of Table 1. The ductility is computed as the ratio of ultimate displacement to the displacement at first yield of internal steel. For computation, the ultimate displacement was set at a displacement corresponding to 20% drops of peak load. This table shows that the application of CFRP sheets has improved the ductility of repaired specimen significantly. Magnitude-wise the increase in ductility for repaired specimen is up to 39% with respect to its original (before repair) specimen.

Stiffness Degradation

The beam-column joint stiffness is estimated by computing the slope of the peak-to-peak line in each loop [9]. Figure 10 shows the stiffness degradation with lateral displacement. This degradation can be attributed to concrete non-linear deformations, flexural and shear cracking, distortion of the joint panel, slippage of reinforcement, loss of cover, debonding or delamination of CFRP etc. A comparison of repaired specimen curve with before repair curve shows that the initial stiffness of repaired specimen is significantly higher than before repair specimen. This high initial stiffness for repaired specimen may be attributed to external bonding of CFRP sheets on beams, joint and column regions. Figure 10 also reveals that, in CFRP repaired specimen, the degradation of stiffness with lateral movement are slow compared to before repair specimen. This is a desirable property in earthquake like situations. It was observed, in the past earthquakes, most of the RC structures failed (or collapsed) due to sudden loss of stiffness of structural joints with increasing lateral movement of the structure.

Figure 10. Stiffness degradation in the specimens.

CONCLUSIONS

The results of the experimental program, presented in this paper, establish the effectiveness of CFRP sheets in repairing and upgrading deficient exterior beam-column joints.  The results of CFRP repaired specimen was compared with its corresponding before repair specimen and, in general, it was observed that CFRP sheets improve the shear resistance and ductility of the RC joint to a great extent.  The failure of CFRP repaired exterior joint due to debonding was examined and it was observed that at higher stages of loading there was significant yielding in beam reinforcing bars that allowed cracks to widen in the beam region which in turn ultimately tore the CFRP sheets.

ACKNOWLEDGEMENTS

Authors acknowledge the financial support provided by King Abdualaziz City for Science and Technology (KACST) under grant Number AR-21-40.

REFERENCES

- Pantazopoulou, S. and Bonacci, J. 1992. “Consideration of questions about beam-column joints,” ACI Structural Journal, 89(1): 27-36.

- Cheung, P.C., Paulay, T., and Park, R. 1993. “Behavior of beam-column joints in seismically loaded R.C. frames,” Journal of The Structural Engineer, 71(8): 129-138.

- Pantazopoulou, S.J., and Bonacci, J.F. 1994. “On earthquake-resistant reinforced concrete frame connections,” Canadian Journal of Civil Engineering, 21: 307-328.

- Hakuto, S., Park, R. and Tanaka, H. 2000. “Seismic load tests on interior and exterior beam-column joints with substandard reinforcing details,” ACI Structural Journal, 97(1): 11-25.

- Hwang, S. and Lee, H. 2000. “Analytical model for predicting shear strengths of interior reinforced concrete beam-column joints for seismic resistance,” ACI Structural Journal, 97(1): 35-44.

- Baglin, P.S., and Scott, R.H. 2000. “Finite element modeling of reinforced concrete beam-column connections,” ACI Structural Journal, 886-894.

- Antonopoulos, C., and Triantafillou, T.C. 2003. “Experimental investigation of FRP-strengthened RC beam-column joints,” Journal of Composites for Construction, ASCE, 7(1): 39-49.

- Ghobarah, A., and Said, A. 2001. “Seismic rehabilitation of beam-column joints using FRP laminates,” Journal of Earthquake Engineering, 5(1): 113-129.

- El-Amoury, T. and Ghobarah, A. 2002. “Seismic rehabilitation of beam-column joint using GFRP sheets,” Engineering Structures, 24:1397-1407.

- Mukherjee, A. and Joshi, M. 2005. “FRPC reinforced concrete beam-column joints under cyclic excitation,” Composite Structures, 17: 185-199.

- Ghobarah, A. and El-Amoury, T. 2005. Seismic rehabilitation of deficient exterior concrete frame joints.  Journal of Composites for Construction, ASCE, 9(1): 408-416.