BEHAVIOR OF CONCRETE BEAMS REINFORCED WITH GFRP BARS UNDER SUSTAINED LOADS AND SEVERE CONDITIONS

Tarek  H. Almusallam

Associate Prof., Dept. of Civil Engineering, King Saud University, Riyadh, Saudi Arabia

Yousef  A. Al-Salloum

Associate Prof., Dept. of Civil Engineering, King Saud University, Riyadh, Saudi Arabia

Saleh  H. Alsayed

Professor, Dept. of Civil Engineering, King Saud University, Riyadh, Saudi Arabia

Abstract

Long-term behavior of composite materials is still a controversial issue among the engineering community though fiber reinforced polymer (FRP) reinforcements are increasingly used in infrastructure applications.  In this paper, the effect of sustained loads on concrete beams reinforced with glass fiber reinforced polymer (GFRP) bars is studied.  The study comprises casting concrete beams reinforced with GFRP bars and subjected to different environments.  All beams were subjected to a certain stress level during their exposure to the environment.  An accelerated aging technique is used to simulate the long-term effect.  The results of this investigation will be very useful to engineers concerned with the design of structures using composite materials.

1. Introduction

In recent years interesting developments have emerged in the field of non-metallic elements as a replacement of steel reinforcement in concrete.  These alternative reinforcements are based on high strength, high modulus artificial fibers, which are embedded in a polymeric resin.  These fibers can be categorized as: glass, aramid, and carbon fibers.  The most impressive characteristic of these non-metallic reinforcement fibers is their chemical stability in environments, which are aggressive to steel (e.g. corrosion).  The available knowledge and experience about application and long-term behavior of the new materials such as glass fiber reinforced polymer (GFRP) bars, is still restricted.  The GFRP bars were used in concrete in the beginning of nineties, mainly in USA and Japan.

The developments were strongly supported by industries operating in the glass composite sector and until recently, worries about durability of glass-based bars in a cementitious environment were almost neglected.  However, excellent mechanical and corrosion resistant characteristics have promoted the use of FRPs in many structural applications all over the world1,2.  Although the short-term mechanical properties of GFRP materials are usually well documented, long-term durability issues still remain.

Most composites exhibit a long-term static strength that is significantly lower than the short-term strength.  This long-term static strength is observed by exposing the material to sustained stress for a long period of time in a certain environmental exposure (i.e. in air, acid, alkaline, sea water at ambient temperature).  The failure due to the degradation of the material properties with time is also referred to as creep rupture.  The loss of strength can be accelerated in adverse environments, such as, in the presence of water, or strong acidic or alkaline solutions.

The long-term static strength of polystal E-glass tendons at 10,000 hours (about 1 year) has been reported to be 70% of the short-term static strength3,4 .  Sultan et al.5 reported that remaining strengths after 10 to 15 years of 40% for hand laid-up fiber glass, and 50% for filament wound composites.  Slattery6 reported that long-term tests on Glass/Epoxy composites showed failure of about half of the samples tested at a sustained stress of only 50% of ultimate, after about 7 years.  Fujii et al.7 tested E-glass composites with relatively brittle polyester matrix.  These composites showed significant matrix microcracking when loaded only 40% of their short-term ultimate strength.  This microcracking resulted in a significant loss of tensile strength (more than 50% in 720 hours) when the composite was immersed in an acidic solution.

Local studies at King Saud University on the durability of GFRP sheets8,9 and GFRP bars10 for unstressed composites have been conducted at different extreme environmental conditions.  The studies showed the strength reduction due to environmental exposure.

The objective of this paper is to investigate the long-term durability of a new generation of GFRP bars under sustained loads in different exposure conditions.  This can be achieved and best represented through testing concrete beams reinforced with GFRP bars and subjected to a certain stress level.  In order to accelerate the reaction, all beams were either completely or partially immersed in different environments (tap-water and sea-water) at elevated temperature.  The results of this investigation will provide a certain confidence level in using GFRP bars in concrete structures taking into account the durability issue (i.e. long-term behavior of concrete beams with GFRP reinforcement).

#### 2. Experimental Program

## 2.1	Beam Details

A total of 36 concrete beams of (100 x 100 x 2000 mm) were prepared for this study.  Each beam was reinforced with 110 mm GFRP bars placed at the tension side (bottom).  No stirrups were provided for all beams in which the concrete was chosen such that the concrete will carry all shear forces without having a chance of shear failure for all beams.  The beam was designed to be loaded with a sustained load, which provided a stress in the GFRP bar equals to 20-25% of its ultimate tensile capacity.  The GFRP bars were coated with high alkali cement paste (40 x 40 x 700 mm) at the middle to increase the alkalinity content around GFRP bars and to allow easy extraction of bars from beams at the day of testing.  The beam cross-section and details are shown in Fig. 1.

## 2.2	Material Properties

The compressive strength of concrete, f'c, was determined by testing standard concrete cylinders that were taken from the mix patch used for all beams after 120 days.  The average value of f'c was 43 MPa.  In order to increase the alkalinity in the paste, Na2O was increased from 0.2% to 1% (about 3.62 kg of NaOH for 350 kg cement).  The specified weight of NaOH pellets were dissolved in the mixing water and then cement added gradually. The average compressive strength of (50 x 50 x 50 mm) paste cubes at the day of testing was about 44.2 MPa.

All beams were reinforced with 10 mm GFRP bars for this study.  The average ultimate tensile strength and strain were measured for the used GFRP bars to be 743 MPa and 0.0187, respectively.  The modulus of elasticity was evaluated from the stress-strain curve to be 39 GPa. The value of ultimate strength was considered as the reference value for tensile strength of GFRP bars.

## 2.3	Beams and Environmental Groups

After casting and curing all 36 beams, they were subdivided into 3 groups based on their environmental exposure.  Each group consisted of 12 beams reinforced with GFRP bars to be exposed to a certain environment.  Three tanks were fabricated for the three groups and painted with an enamel paint for protection and fitted with electrical heaters and thermostat to control the temperature of water to about 40 C.  The tanks were designated as T1 (for tap water continuous exposure at 40 C), T2 (for sea water continuous exposure at 40 C), and T3 (for wet/dry cycles every 2 weeks in sea water exposure at 40 C).  Each tank contains 12 beams, in which 6 beams were unloaded and the other 6 were loaded with sustained dead loads of about 230 kg on each.

## 2.4	Preparation of Test Specimens

All beams were prepared such that the GFRP bars can be extracted easily from beams with minimal damage to the bars.  This was achieved by casting the cement paste (with high alkalinity) around the middle part of the GFRP bars as shown in Fig. 1.  Also all bars were connected with 3 strain gages at the middle part of each bar embedded in all beams for the strain measurements during loading.  These strain measurements in the GFRP bars were taken in order to study the stress-strain behavior of GFRP bars after environment exposure under sustained loads and will be reported in another study.  Four beams (2 unloaded and 2 loaded) from each tank were scheduled for each age of testing (4, 8 and 16 months).

- Beam set-up

(b) Beam cross-section (Section A-A)

Fig. 1.  The beam specimen details

#### 3. Test Results

## 3.1	Tension Test Results

After 4, 8 and 16 months of exposure in all environments, four beams from each environment (2 unloaded and 2 loaded) were removed from tanks to prepare samples for testing.  The GFRP bars were extracted carefully from all beams and two samples of GFRP bars were taken from each beam to be ready for tension test.  Uniaxial tension tests were performed on the stressed and unstressed GFRP bars using 500 kN capacity universal testing machine, with specially modified grips consists of two split steel pipes used for gripping the bars after sand coating at both ends.  Bars were tested as received directly from the manufacturer without simulating any environmental or loading effects.  Data obtained from these bars were utilized as a basis (control) for evaluating the performance (reduction in tensile strength) of conditioned and stressed bars.  The tensile average strength values for stressed and unstressed tested samples for all bars after 4, 8 and 16 months of exposure are given in Table 1.  It is clear from Table 1 that the maximum reductions in tensile strength for wet/dry seawater exposure at 40C, after 4, 8 and 16 months for unstressed specimens were about 10%, 17% and 22%, respectively.  However, the maximum reductions in tensile strength for unstressed specimens, continuously immersed in tap-water for 4, 8 and 16 months exposure at 40C were about 5%, 13% and 16%, respectively.  Also, the maximum reductions in tensile strength for unstressed specimens, continuously immersed in seawater for 4, 8 and 16 months exposure at 40C were about 2%, 16% and 20%, respectively.  For specimens with stressed GFRP bars (20-25% of their ultimate), the maximum reduction in tensile strength after 4 months of continuous conditioning in seawater at 40C was about 30%, while the maximum reduction after 8 and 16 months exhibited for wet/dry sea-water exposure at 47% and 55% reductions, respectively.  The other reduction values can be observed clearly from Table 1 for 4, 8 and 16 months exposure period.

## Table 2. Tensile strength test results after 4 ,8 and 16 months

| Exposure Condition | Loading Condition | 4 months Exposure |  | 8 months Exposure |  | 16 months Exposure |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | fu (MPa) | Reduction (%) | fu (MPa) | Reduction (%) | fu (MPa) | Reduction (%) |
| Control (un-conditioned | Unstressed | 743 | -- | 743 | -- | 743 | -- |
| Tap water (40 C) | Unstressed | 707 | 4.9 | 646 | 13.1 | 622 | 16.3 |
|  | Stressed (20-25%) | 536 | 27.9 | 463 | 37.7 | 393 | 47.1 |
| Sea water (40 C) | Unstressed | 728 | 2.1 | 627 | 15.6 | 597 | 19.7 |
|  | Stressed (20-25%) | 525 | 29.4 | 453 | 39.0 | 387 | 47.9 |
| Sea water wet/dry (40 C) | Unstressed | 667 | 10.3 | 617 | 17.0 | 581 | 21.8 |
|  | Stressed (20-25%) | 537 | 27.8 | 394 | 47.0 | 334 | 55.0 |

## 3.2	Load-Deflection Behavior

Additional stressed and unstressed beams were prepared and placed in T1 and T3 tanks and then tested for flexure after 4 and 8 months in order to study the effect of environments and sustained loads on the load-deflection behavior of conditioned beams reinforced with GFRP bars.  Figs. 2 and 3 shows the load deflection curves for the beams tested for flexure from the considered exposure conditions.  Each figure shows the reduction in load capacity, stiffness and deflection due to exposure and loading conditions for all unstressed and stressed beams after 4 and 8 months of exposure. In most cases the load capacity and deflection reductions at ultimate were exhibited for stressed beams after 8 months of exposure for all environments.  The same trend was observed for unstressed beams after 8 months of exposure.  Some of unstressed samples such as T1B5 in Fig. 2 exhibited higher initial stiffness than T1B1.  This is attributed to the gain in concrete strength between 4 and 8 months of exposure in tap water.  Also it can be observed from most of the curves that all stressed beams exhibited higher stiffness after 4 and 8 months of exposure than unstressed samples at high load levels.

Fig.  2.  Load-deflection relationships for beams tested after 4 and 8 months of exposure in Tank 1 (tap-water continuous exposure at 40C)

## Fig. 3. Load-deflection relationships for beams tested after 4 and 8 months of exposure in Tank 3 (wet/dry seawater exposure at 40C)

There is no obvious reason for such observation.  However, it seems that for stressed beams the combination effect of creep and loading may lead to higher stiffness at high load levels.

# 4.	Conclusions

The laboratory test results presented in this study clearly show that there are significant losses (about 27-29% after 4 months, 37-47% after 8 months and 47-55% after 16 months) in tensile strength of GFRP bars when subjected to sustained stress of about 20-25% of their ultimate for the three environments considered in this study.  The loss in tensile strength of the unstressed specimens under the same environments ranges between 2-10% after 4 months, 13-17% for 8 months and 16-22% for 16 months of exposure.  It is clear that the degradation in the GFRP bars is significant when the bars were subjected to sustained stress for a period of time.  Similar losses in the flexural strength of these beams were noticed.  However, further studies are required in order to come up with solid conclusions.

##### 5.	Acknowledgments

The authors gratefully acknowledge the financial support received from Saudi Arabian Basic Industries Corporation (SABIC) to execute the presented study.

##### 6.	References

1.	Malvar, L.J., "Literature Review of Durability of Composites in Reinforced Concrete," Special Publications SP-2008-SHR, Naval Facilities Engineering Service Center, Port Hueneme, CA, 1996.

2.	Nanni, A. (editor), Fiber-Reinforced-Plastic (FRP) Reinforcement for Concrete Structures: Properties and Applications, Developments in Civil Engineering, 42, Elsevier Science Publishers, 1993.

3.	Wolff, R. Miesseler, H.J., "New Materials for Prestressing and Monitoring Heavy Structures," Concrete International, 1989, Vol. 11, No. 9, pp. 86-89.

4.	Taerwe, L., "FRP Developments and Applications in Europe," Fiber-Reinforced- Plastic (FRP) Reinforcement for Concrete Structures: Properties and Applications, Developments in Civil Engg., 42, A. Nanni ed., Elsevier Science Publishers, 1993, pp. 99-114.

5.	Sultan, M. Hawkins, G., Sheng, L.H., "CALTRANS Program for the Evaluation of Fiber Reinforced Plastics for Seismic Retrofit and Rehabilitation of Structures," Proceedings of FHWA National Seismic Conference, San Diego, CA, 1995.

6.	Slattery, K., "Mechanistic Model for the Creep-Rupture Process in Filamentary Composites," Infrastructure: New Materials and Methods of Repair, Proceedings of the Third Materials Engineering Conference, San Diego, CA, 1994, pp. 215-222.

7.	Fujii, Maekawa, Z., Hamada, H., Kubota, T., Murakami, A.and  Yoshiki, T., "Evaluation of Initial Damage and Stress Corrosion of GFRP," 9th Intl. Conf. on Composite Materials (ICCM/9), Madrid, Spain, 1993, Vol. 5, pp. 562-568.

8.	Almusallam, T.H., Al-Salloum, Y.A. and Alsayed, S.H., “Behavior of Concrete Cylinders Confined with GFRP Sheets in Severe Environmental Conditions,” Proceedings of the Third International Conference on Concrete Under Severe Conditions: Environment & Loading (CONSEC’01), Vancouver, Canada, June 18-20, 2001.

9.	Al-Salloum, Y.A., Almusallam, T.H. and Alsayed, S.H., “Effect of Hot-Dry Weather on Performance of RC Beams Externally Strengthened with GFRP Sheets,” Proceedings of the Third International Conference on Concrete Under Severe Conditions: Environment & Loading (CONSEC’01), Vancouver, Canada, June 18-20, 2001.

10.	Alsayed, S. and Alhozaimy, A., “Effect of High Temperature and Alkaline Solutions on the Durability of FRP Bars,” Proceedings of the First International Conference on Durability of Fiber Reinforced Polymer (FRP) Composites for Construction (CDCC’98), Sherbrooke, Canada, August 5-7, 1998, pp. 623-634.