## Slide 1: Prof. Mohamed El-Newehy King Saud University Chemistry Department, College of Science http://fac.ksu.edu.sa/melnewehy/home
CHEM 342 POLYMERS AND PETROCHEMICALS FOR CHEMISTRY’ STUDENTS, COLLEGE OF SCIENCE PRE-REQUISITES COURSE; CHEM 241 CREDIT HOURS; 2 (2+0)

## Slide 2
POLYMER REACTIONS AND MODIFICATION

## Slide 3
REACTIONS OF SYNTHETIC POLYMERS
Polymer can be chemically modified to improve some property, such as biocompatibility, fire retardancy, or adhesion, or to provide specific functional groups for ion-exchange or other applications.
Example;
Bromination is sometimes used to impart fire retardancy to some polymers.
Poly(vinyl chloride) can be chlorinated after polymerization to increase its softening temperature or to improve its ability to blend with other polymers.
Important commercial polymers can be produced only by the chemical modification of a precursor polymer.
Examples;
Poly(vinyl alcohol), poly(vinyl butyral), cellulose derivatives such as cellulose acetate and cellulose nitrate, and polyphosphazenes—an interesting group of inorganic polymers.

## Slide 4
CHEMICAL MODIFICATION
Chloromethylation of polystyrene, by reacting with a chloromethyl ether in the presence of a Friedel-Crafts catalyst like aluminum chloride, AlCl3, can be used to introduce functionality such as aldehyde or carboxylic acid groups in polystyrene.
Aldehydes serve to form a Schiff base with protein amines.
Highly chloromethylated PS can be quaternized with tertiary amines to yield water-soluble polymers, ionomers, and ion-exchange resins.
Chloromethylated PS also can be reacted with a phosphide to introduce phosphinic ligands for binding metal coordination complexes in the preparation of polymer-bound catalysts.
Chloromethylation
Chloromethylation of polystyrene.

## Slide 5
CHEMICAL MODIFICATION
The surface of a polymer can be modified to provide sites for immobilization of enzymes or other biopolymers or to improve the solvent resistance or biocompatibility of a polymer.
Plasma activation is one approach to modify polymer surfaces.
Another method is direct fluorination, oxidation, nitration, and sulfonation.
Example;
The surface of a hydrocarbon polymer such as polyethylene or polypropylene can be fluorinated by exposure to 5% to 10% fluorine gas diluted in nitrogen for one to 15 min.
The fluorinated surface provides hydrophobicity, oxidation resistance, and solvent resistance for applications such as plastic fuel tanks and rubber gloves.
Surface Modification

## Slide 6
CHEMICAL MODIFICATION
Cation-exchange resins possess a fixed negative charge and exchange cations such as Ca2+, Na+, and H+.
Anion-exchange resins possess a positive charge on the functional group or are positively charged during the ion-exchange reaction during which anions such as HCO3–, SO4–, and OH– are exchanged.
Most ion-exchange resins are prepared by suspension polymerization of monomers such as styrene.
Example;
Crosslinked polystyrene can be obtained by incorporation of a few percent of a difunctional comonomer such as divinylbenzene.
The resulting beads are macroporous and can be used as a column packing.
Ion-Exchange Resins
Functionalization can be obtained by different chemical routes, such as sulfonation, chloromethylation, amino-methylation, aminolysis, and hydrolysis.

## Slide 7
CHEMICAL MODIFICATION
Example; Sulfonation of A Crosslinked Polystyrene Bead
A cation exchange resin can be prepared by sulfonation of a crosslinked polystyrene bead in concentrated sulfuric acid with an organic solvent, such as dioxane.
Sulfonation primarily occurs at the para-position with some ortho-substitution.
Ion-Exchange Resins
A strongly acidic cation-exchange resin prepared from polystyrene.
Example;
A styrenic anion-exchange resin can be prepared by reacting the benzyl chloride of chloromethylated polystyrene with a tertiary amine, N(CH3)3.
A strongly basic anion-exchange resin prepared from polystyrene.

## Slide 8
CHEMICAL MODIFICATION
These addition reactions of unsaturated polymers, like liquid polybutadiene, developed into preparations of useful commercial materials.
Hydrogen peroxide or peracetic acid is used in the presence of organic acids or their heavy metal salts.
Epoxidation Reactions
The reaction is accompanied by formations of by-products:

## Slide 9
REARRANGEMENT REACTIONS
The isomerization of cis-polybutadiene can be carried out with the aid of ultraviolet light or with
gamma radiation.
When light is used, the free-radical reaction requires photoinitiators.
The mechanism involves freely rotating transitory free-radicals on the polymer backbone.
These form from additions of photoinitiator fragments to the double bonds.
The adducts break up again, releasing the attached initiator fragments and reestablishing the double bonds.
The new configurations are trans because they are more thermodynamically stable.
Isomerization Reactions
where, X• represents a free-radical fragment from a photoinitiator.

## Slide 10
REARRANGEMENT REACTIONS
With gamma radiation, there is no need for any additives.
The mechanism of isomerization is believed to involve direct excitation of the p-electrons of the double bonds to antibonding orbitals where free and geometric interconversions are possible.
In benzene solutions, energy transfers take place from excited benzene molecules to the polymer double bonds.
Isomerization Reactions
Example; When 1,4-polyisoprene films are irradiated with light, cis–trans isomerizations occur.

## Slide 11
PREPARATION OF POLYMER DERIVATIVES
Cellulose, which can be obtained from wood pulp and short fibers left from cotton recovery, is one of nature's most abundant biopolymers.
A typical chain is composed of 2,000 to 6,000 anhydro glucose units (typical molecular weight of 300,000 to 1,000,000) each of which contains three hydroxyl groups and is linked by an acetal bridge.
The rigid chain of cellulose is strongly hydrogen bonded and highly crystalline.
For these reasons;
Cellulose is essentially insoluble and infusible (degrades before melting), and therefore fibers and films can be obtained only by chemically modifying cellulose.
Regeneration process; Cellulose fiber (rayon) or film (cellophane) can be obtained by the viscose process.
In this process, cellulose pulp is first reacted with carbon disulfide to form cellulose xanthate, which is soluble in a caustic solution.
Cellulose xanthate is then converted back to cellulose (regeneration) by treatment with aqueous sulfuric acid.
Cellulose

## Slide 12
PREPARATION OF POLYMER DERIVATIVES
Preparation of cellulose acetate from cellulose.
For simplicity, lone hydrogen atoms on the cellulose repeating units are omitted.
Cellulose

## Slide 13
PREPARATION OF POLYMER DERIVATIVES
Various soluble cellulose derivatives can be obtained by chemical modification of the hydroxyl groups.
Cellulose acetate,
It can be obtained by reacting cellulose with glacial acetic acid in the presence of acetic anhydride and traces of sulfuric acid in refluxing methylene chloride.
Cellulose triacetate (CTA); If all the hydroxyl groups are reacted, which can be wet spun into fiber (acetate) from a methylene chloride–alcohol solvent mixture.
Cellulose diacetate; It can be obtained by partially hydrolysis of cellulose triacetate in which two (secondary) of the three hydroxyl groups in each anhydro glucose unit remain acetylated.
In commercial grades of cellulose acetate, about 65% to 75% of all available hydroxyl groups remain acetylated.
This polymer is amorphous and highly soluble in many solvents including acetone, from which it can be dry spun.
Cellulose

## Slide 14
PREPARATION OF POLYMER DERIVATIVES
Poly(vinyl alcohol) (PVA) is obtained by the direct hydrolysis (or catalyzed alcoholysis) of poly(vinyl acetate) (PVAC):
Poly(vinyl alcohol)
Poly(vinyl acetate) is produced by free-radical emulsion or suspension polymerization.
Poly(vinyl acetate) has a low glass-transition temperature (29C) and finds some applications as an adhesive.
Poly(vinyl alcohol), which is used as a stabilizing agent in emulsion polymerizations and as a thickening and gelling agent, cannot be polymerized directly because its monomer, vinyl alcohol, is isomeric with acetaldehyde

## Slide 15
PREPARATION OF POLYMER DERIVATIVES
Poly(vinyl butyral) (PVB), which is used as the film between the layers of glass in safety windshields, is obtained by partially reacting PVA with butyraldehyde.
For safety-glass applications, approximately 25% of the repeating units of PVA are left unreacted to promote adhesion to the glass through interaction of the hydroxyl group with the surface (i.e., silanol) groups of the glass.
Poly(vinyl butyral)
Production of poly(vinyl butyral) from a poly(vinyl alcohol) precursor.