## Slide 1: Influences of Poly(Vinyl Alcohol) Molecular Weight and Carbon Nanotubes on Radiation-Crosslinking Shape Memory Polymers
Aamer A. M. Alfayyadh

## Slide 2: Introduction
Overview of Shape Memory Polymers (SMPs):
  Ability to return to original shape upon external stimulus.
  Applications in various fields like aerospace and dynamic molds.

## Slide 3: Objectives of the Study
To prepare and characterize chemically and radiation-crosslinked PVA/CEA nanocomposites.
To investigate the effects of molecular weight and carbon nanotubes (CNTs) on properties.

## Slide 4: Materials and Methods
Materials Used:
  PVA of two molecular weights (16,000 g/mol and 146,000 g/mol).
  2-Carboxyethyl Acrylate (CEA), MWCNT, and MWCNT-NH2.
Methods:
  Chemical crosslinking with glutaraldehyde.
  Radiation crosslinking using gamma irradiation.

## Slide 5: Gel Content Analysis
  Gel content increases with irradiation dose and filler concentration.
  Higher molecular weight PVA yields lower gel content compared to lower molecular weight.

## Slide 6: Swelling Behaviour
  Swelling remains below 1%, indicating effective crosslinking.
  Minimal swelling attributed to bound water and increased filler concentration.

## Slide 7: Morphology Observation
  Homogeneous distribution of fillers in the polymer matrix.
  Presence of pores and surface texture variations due to fillers.

## Slide 8: Thermogravimetric Analysis (TGA)
  Three weight loss stages indicate degradation processes.
  Higher molecular weight PVA shows decreased thermal stability with increased irradiation.

## Slide 9: Dynamic Mechanical Analysis (DMA) - Tan Delta
  Tan δ increases with the addition of MWCNT and MWCNT-NH2, indicating enhanced material response to thermal changes.

## Slide 10: Storage and Rubbery Moduli
  Storage modulus decreases with increased irradiation.
  MWCNT-filled composites exhibit better mechanical properties than those without fillers.

## Slide 11: Loss Modulus
  Higher loss modulus values for irradiated samples, indicating improved energy dissipation.

## Slide 12: Shape Memory Effect
  Demonstrates the ability of the material to recover its original shape after deformation.

## Slide 13: Conclusions
  Successful preparation of PVA nanocomposites with enhanced properties.
  The addition of MWCNT and MWCNT-NH2 improves mechanical and thermal properties.